INFORMATION ON DOCTORAL THESIS

1. Full name:	Vu Minh Thanh

2. Sex: Male

3. Date of birth: February 22th 1980

4. Place of birth: Thai Binh

5. Admission decision number: 4374/QD-DHKHTN-CTSV date 3/12/2012 by the Rector of VNU University ò Science

6. Changes in academic process: Non

7. Official thesis title: Study on manufacture of carbon nanotube fiber reinforced carbon-carbon composites for application in high technology fields

8. Major: Theoretical Chemistry and Physicochemistry

9. Code: 60 44 01 19

10. Supervisors: 1. Associate Professor, PhD Le Kim Long;  2. Professor, PhD Nguyen Duc Nghia

11. Summary of the new findings of the thesis

- Determined the optimum conditions for fabrication of CCC through investigating    the pyrolysis process of the CCC preform using TGA technology.

- Determined effects of CNT on the pyrolysis, carburization and heat treatment processes of the CCC.

- Determined the main factors that affect the film-forming process as well as chose the conditions suitable for synthesis of the anti-oxidant ZrC coating film at high temperature for the surface of the CCC.

- Fabricated the high density CNT-contained CCC with good thermal shock and wear resistance and anti-oxidant at high temperature (>2500oC), which could give potential applications in high technology fields for national security, defense and economy.

12. Paratical applicability, if any:

13. Further research directions, if any

14. Thesis-related publications:

[1] Van Thu Le, Cao Long Ngo, Quoc Trung Le, Trinh Tung Ngo, Duc Nghia Nguyen and Minh Thanh Vu (2013), "Surface modification and functionalization of carbon nanotube with some organic compounds", Advances in Natural Sciences: Nanoscience and Nanotechnology 4 (3), pp. 1-5.

[2] Vu Minh Thanh, Dang Van Duong, Le Kim Long and Nguyen Duc Nghia (2014), "Synthesis and properties of zirconium carbide film on graphite", Journal of Chemistry, 52 (2), pp. 157-162.

[3] Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Le Van Thu, Dang Van Duong, Doan Tuan Anh, Pham Tuan Anh (2014), "Synthesis and properties of composites based on graphite powder, carbon fiber and carbon nanotube", The 7th International Workshop on Advanced Materials Science and Nanotechnology (IWAMSN2014), pp. 390-395.

[4] Vu Minh Thanh, Le Kim Long, Nguyen Đuc Nghia, Pham Tuan Anh, Đoan Tuan Anh, La Van Tha (2015), "Effect of heat treatment conditions on Culon-500 carbon fiber surface properties and fibers/resin matrix composite interfacial adhesion", Journal of Research Science and Technology Military, 38, pp. 116-122.

[5] Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Pham Tuan Anh, Doan Tuan Anh, Le Van Thu (2015), "The influence of temperature - programmed decomposition treatment on microstructure and thermal properties of the graphite powder - carbon fiber - carbon nanotube - phenolic resil composite", Journal of Science and Technology 53(1A), pp. 192-198.

[6] Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia (2015), "Effect of treatment temperature on carbon fiber surface properties reinforced carbon-carbon composites", Journal of Science and Technology 53(1A), pp. 270-278.

[7] Doan Tuan Anh, Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Pham Tuan Anh, Le Van Thu, Nguyen The Huu (2015), "Investigation on effecting factors on properties of materials using as preform for carbon/carbon composite fabrication", Journal of Research Science and Technology Military, 10, pp. 14-19.

[8] Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Pham Tuan Anh, Doan Tuan Anh, Le Van Thu, Ho Ngoc Minh, Nguyen Manh Tuong (2015), "Modification and effect of multi-walled carbon nanotube on thermal properties of phenolformaldehyde resil", Journal of Research Science and Technology Military, 10, pp. 153-160.

[9] Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Ngo Minh Tien, Đang Van Đuong, Ngo Quoc Dung (2015), "Study on effects of heat-treatment process to structure and properties of carbon-carbon composite", Journal of Chemistry, 53(5A), pp. 141-146.

[10] Pham Tuan Anh, Vu Minh Thanh, Le Kim Long, Nguyen Duc Nghia, Doan Tuan Anh, Le Van Thu (2015), "The influence of the chemical vapor infiltration process of carbon on the carbon/carbon material properties", Journal of Chemistry, 53(5A), pp. 182-188.